Protocol for using digital mask to fabricate SU-8 device masters

Print Alignment Manifold

The manifold was printed using Elegoo ABS-like resin according to the manufacturer’s guidelines. The assembly of the complete device is shown in Figure 1 of the supplementary documents in the paper.

- Set up the correct settings: Choose ELEGOO Saturn 4 profile and import the resin settings for the specific resin you are using.

- Import the model into the slicer: Go to "File" > "Open File", select your model and click "Open".

- Orient the model: Place it at a proper angle on the build plate to reduce the support contact area and improve resin flow. The surface with more details should be oriented upwards. Otherwise, support structures may obscure the features.

- Add supports: Resin prints require supports to hold overhanging parts. Click "Support", then click "Generate Automatic Supports" to add support for the model's overhanging area.

- Slice and export: Click "Slice" and "Save Sliced File". Then Click "Confirm" to save the file to a USB. You can save the file as .goo file.

- Add the resin: The resin may settle after prolonged standing. It is recommended to shake the resin bottle before use. Pour the resin into the tank and make sure not to exceed the maximum fill line of the tank.

- Start the print: Insert the USB drive to the printer and initiate the print. Keep the cover closed while printing.

- Remove the print carefully: Put the resin tray at the designated mounting position. Remove the build plate and use the shovel to detach the model from the build plate.

- Remove supports: Use diagonal pliers to carefully cut supports without damaging small components.

- Wash in isopropyl alcohol (IPA) or resin cleaner: Soak or gently agitate the model for 2-5 minutes to remove uncured resin.

- Dry the print: Let the print air dry or use compressed air to avoid water or alcohol marks.

- Sand the print: Cut off leftover supports in detailed or hidden areas. Use sandpaper to smooth out any remaining support marks.

- Post curing the model with 405 or 365nm light to fully harden the model and improve strength and stability.

- Drain the resin from the tank: Place the resin bottle on the resin filtering and collection rack and put on paper funnels (if you have). Remove the tank mounting screw. Pour the resin through the funnel. Use a plastic scraper to clean the remaining resin in the resin tank.

- Spray a moderate amount of alcohol into the tank and wipe it clean with tissues.

- Clean the build plate: Remove the build plate and spray it with alcohol. Wipe off any remaining resin with tissues.

Sources protocol: How to Do Resin 3D Printing - Beginner's Guide – ELEGOO Official

Preparing Digital Mask on 3D Printer (Elegoo Saturn 4 / Mars 5)

Design The File

  - Open the CAD software of your choice (AutoCad, Solidworks, Creo, etc.)

  - Draw the sketch where all the features will be extruded to the same height, with the reference dimensions and distance should follow the calibration print for the same SU-8 thickness (calibration print file has been provided in supplement files).

Figure 1 Example for mask drawing on CAD software using CREO 12

  - Save the file in .stl format with the highest details set.

  - Open the slicer software of the 3D printer and import the model

  - Reorientation the model so it can be stay on the middle of the printer LCD, where all the features should lay parallel to the LCD screen.

Figure 2 Correct orientation for printing the 3D printed Su-8 mask on LCD screen.

  - Set up the printer as below and slice the model to get the .goo file

  - Import it to the 3D printer and print.

Attention:

- Printing dimensions should be maintained in millimeters (mm). Using units other than mm or inches may cause the slicer software to malfunction, resulting in missing models or inaccurate dimensions.

Setup the LCD mask

- After setting up the printer in the software, configure the printer parameters as shown below.

Figure 3 Basic settings for SU-8 printing using Elegoo Voxeldance Tango 4.0

All parameters should remain unchanged except for the exposure setting, which must be adjusted according to the SU-8 thickness.

To estimate the total printing time:

Printing Time=Model HeightLayer Height×Exposure Time

where:

- Model Height is obtained from the sketch,

- Layer Height is shown in the top-left corner,

- Exposure Time is found under Common Layer Settings on the right panel.

- In the Advanced Panel, modify the default settings for the Saturn 4 printer as shown below.

Figure 4 Advanced settings for SU-8 printing using Elegoo Voxeldance Tango 4.0

Modification of SU-8 with ITX

Materials Required

- SU-8 Photoresist (SU-8 3000 series - Kayaku AM): 10 g

- Isopropylthioxanthone (ITX, TCI – CAS: 5495-84-1): 0.1 g

- Analytical balance (accuracy: 0.001 g)

- Glass vial (15-20 mL capacity)

- Handheld mixer

- Protective gloves, goggles, and lab coat

Procedure

- Weigh 0.1 g of ITX using an analytical balance and transfer it to a clean glass vial.

- Weigh 10 g of SU-8 and transfer it into the clean vial to get 1%w/w of ITX in SU-8.

- Stir components together by using the handheld mixer

- To remove any trapped air bubbles, place the mixture in a vacuum chamber or use an ultrasonic bath for degassing.

- Degas for 1 - 2 hours until no visible bubbles remain or keep in the cabinet for 1 – 2 days before use.

- Store the solution in a cool, dry place, away from light.

Fabrication of SU-8 master with digital mask

Required Equipment

- 1 × Pyrex dish of appropriate size (minimum area: at least 2× larger than the wafer)

- 1 × Tweezers

- 1 × Hotplate

- 1 × Spin coater

- 1 × Glass slide

- 1 × Printing file consisting of a rectangle matching the LCD size of the printer using the default mask design settings

- 1 × Wash bottle containing IPA

- 1 × Wash bottle containing PGMEA

- 1 × Plasma treatment device (corona treater)

Fabrication Procedure

- Take a glass slide from storage and clean it thoroughly with IPA.  (For a silicon wafer, skip to step 9)

- Blow dry the glass slide using an empty squeeze bottle or compressed air from the laboratory air nozzle.

- Pretreat the glass surface using a corona treater, then place the slide at the center of the spin coater.

- Pour an adequate amount of ITX-SU-8 onto the center of the glass slide (approximately the size of a 1-dollar coin, ~26.5 mm in diameter)

- Spin at the highest RPM speed to coat a thin layer of SU-8 on the glass

- Turn on the hotplate and set the temperature to 80°C

- Soft bake at 80°C for 10 minutes

- Expose the slide to 405 nm light for 200s to generate a uniform first layer

- Pour an adequate amount of ITX-SU-8 onto the center of the glass slide

- Select the appropriate spin-coating RPM according to the desired SU-8 thickness based on the manufacturer’s guidelines.

- Pour an adequate amount of ITX-SU-8 onto the center of the glass slide

- Transfer the coated glass slide onto the hotplate for soft baking.
The baking duration should be 1.5× longer than the manufacturer’s recommended baking time at 95°C for the corresponding SU-8 thickness.

- Remove the glass slide and place it onto the manifold as described in Figure 3A of the paper.

- Insert the USB drive into the 3D printer USB port and select the printing file.

- Wait a few seconds until the two warning prompts appear, then bypass them.

- After printing the first layer, remove the glass slide from the printer and place it back onto the spin coater to coat the second SU-8 layer with the desired thickness.

- Perform the soft bake again using the same condition:

- baking time = 1.5× the manufacturer’s recommended time at 95°C.

- Carefully reposition the glass slide onto the manifold. Push the slide gently toward one corner of the manifold to ensure alignment before printing the second layer.

- After printing the second layer, perform a post-exposure bake at 95°C for 30 seconds.

- Submerge the slide in a Pyrex dish containing PGMEA developer solution.

- Develop the slide by gently shaking the dish in an orbital motion for approximately 5–10 minutes, or until the microfeatures become clearly visible.

- Rinse the slide with IPA.

- If a white residue appears, rinse again with PGMEA before applying IPA once more.

- Blow dry the slide thoroughly.

- Store the fabricated SU-8 mold in an appropriate container for subsequent PDMS casting.